### PART 1 - GENERAL

- DESCRIPTION

  - Work included:

    - Steel double weatherstripped lift and slide door and frame configurations.

    - All window anchors, mullions, covers and trim.

    - Factory applied Hope’s Power of 5 Finishing System.

  - Related work specified elsewhere:

    - Glass, glazing and glazing materials, Section 08810.

    - Perimeter caulking, Section 07915.

    - Miscellaneous structural items, Section 05100.

- QUALITY ASSURANCE

  - Manufacturer shall have not less than 10 years experience in the fabrication of heavy custom steel doors and be a member of The Steel Window Institute (SWI).

  - Installation of doors shall be done by experienced door installers.

  - Allowable tolerances: Size dimensions + 1/16 inch.

  - Source quality control:

    - All doors shall comply with the International Building Code (IBC), the International Residential Code (IRC), the Florida Building Code (FBC) and the Dade County Product Control Division.

    - Air infiltration test

      - Products must be independently lab tested and meet or exceed ASTM E283 or Miami-Dade Testing Application Standard TAS 202.

      - Maximum air infiltration 0.34 CFM/SQ Ft. with differential pressure across window unit of 1.57/ 6.24 PSF.

    - Water penetration test

      - Products must be independently lab tested and meet or exceed ASTM E331 or Miami-Dade TAS 202.

      - No water penetration for 15 minutes when window is subjected to a rate of flow of 5 gal./hr./sq. ft. with differential pressure across window unit of 4.50 PSF (or 15% design pressure for areas requiring HVHZ).

    - Field test

      - Field testing criteria (when applicable) shall be in accordance with AAMA 502-12

    - Structural test

      - Meets or exceeds ASTM E330 or Miami-Dade TAS 202.

    - Forced entry test

      - Meets or exceeds ASTM F588 or Miami-Dade TAS 202.

      - Grade 40 @ 300 pounds

    - Impact test – Large missile

      - Meets or exceeds FBC ASTM E1996 or Miami-Dade TAS 201.

      - Withstand 2x4 missile impact at all designated contact points without penetration.

    - Cyclic wind loading test

      - Meets or exceeds FBC ASTM E1886 or Miami-Dade TAS 203.

      - No failure or distress after subjected to the cyclic sequence to a design load (positive and negative.)

    - Quality of Power of 5 finishing process shall meet or exceed the following designations:

      - Paint Blistering:  ASTM D714.

      - Humidity:  ASTM D4585.

      - Salt Spray (Fog):  ASTM B117.

      - Painted Products in Corrosive Environments:  ASTM D1654.

      - Cyclic Fog/Dry (Prohesion):  ASTM G85.

      - Slat Fog/UV Painted Metal:  ASTM D5894.

      - Pull off Strength of Coating:  ASTM D4541.

    - Upon request, the window manufacturer shall provide a test report from a qualified independent U.S. testing laboratory regularly engaged in testing windows to verify that products conform to test requirement as outlined.

- SUBMITTALS

  - Samples (as requested by architect):

    - Typical 6" door profile with glazing beads.

    - Sample of specified muntin, showing welded intersections and glazing beads.

    - Color sample of finish.

    - Hardware.

  - Shop drawings and manufacturer's literature:

    - Submit for approval shop drawings showing door and installation details, including anchorage, fastening and recommended sealing methods.

    - Dimensioned elevations showing door opening and door sizes.

    - The manufacturer shall not commence any work until shop drawings have been approved.

    - Color charts for finishes.

- PRODUCT, STORAGE AND HANDLING

  - The General Contractor shall be responsible for the protection and storage of the doors after delivery to the site.

  - Store in designated areas in an upright position on wood slats or on a dry floor in a manner that will prevent damage.  Ventilate canvas or plastic coverings to prevent humidity buildup.

- WARRANTY

  - Provide Hope’s standard 10 year Limited Warranty.

PART 2 - PRODUCT AND FABRICATION

- Manufacturers:

  - Furnish all labor and materials to complete the fabrication of doors as shown on architect's drawings and as specified herein.  All doors covered by this specification shall be domestically manufactured in the U.S.A.

  - Manufacturers:  Subject to compliance with requirements covered in this specification, provide products by Hope’s Windows, Inc. – Jamestown, NY (phone: 716-665-5124, e-mail: sales@hopeswindows.com) whose name and products are used to establish the standard of workmanship.

  - Substitutions:  Written approval necessary 10 days prior to bid through submission of the following:

    - Full-size window/door samples matching required scope.

    - Applicable test reports as outlined in Quality Assurance Section 1.2

    - List of (5) recently completed projects of similar size and scope.

- MATERIALS

  - Door and frames shall be manufactured from 12 gauge steel.

  - Muntins (select from items 1 or 2 below):

    - True Divided Lite muntins:

      - Muntins shall be manufactured from solid hot-rolled steel, size to be determined by design.

      - Glazing rebate surfaces must be perpendicular to the stem of this profile.  Rebate surfaces that are tapered will not be acceptable.

      - 1-3/4” tee shall weigh 1.62 pounds per lineal foot, the 1-3/8” tee shall weigh 1.44 pounds per lineal foot and the 7/8” tee shall weigh 1.19 pounds per lineal foot (specify).

      - All steel muntin profiles must be a minimum of 1-3/4″ in depth.

    - Simulated Divided Lite muntins  (select from items below):

      - Hot-rolled stainless steel muntin - #84H profile shall be solid hot rolled from stainless steel with tapers rolled integral at the mill. #84H muntins shall be solidly welded to perimeter framing and dressed smooth. Opposite side muntin shall be extruded aluminum Alloy 6063-T5 matching the profiles as detailed.

      - Interior/exterior muntin - Profiles shall be extruded aluminum Alloy 6063-T5 matching the profiles as detailed.

  - Hardware and weatherstrip adaptors shall be extruded aluminum Alloy 6063-T5 with a minimum thickness of .100 inches.

  - Weatherstripping shall be extruded vinyl, EPDM closed cell sponge, flexible silicone or polyethylene clad urethane foam.

  - Glazing beads shall be extruded aluminum Alloy 6063-T5 with a minimum thickness of .062 inches.

  - Hardware reinforcements shall be 7, 10 or 12 gauge to suit specified hardware.

  - All screws that are furnished by Hope’s, for hardware, trim, covers, anchoring, weather bars, water dams, screens, etc. shall be non-ferrous brass or stainless steel.  Glazing bead screws are plated steel.

  - Power of 5 Finishing:

    - Cleaning.

    - Pretreatment.

    - Epoxy E-Coat primer.

    - Epoxy powder primer.

    - Ultrathane polyurethane top coat.

- FABRICATION

  - Fabricate steel doors in accordance with approved shop drawings.

  - Perimeter frame corners shall be coped and fully welded for maximum strength and weather-tightness with face welds dressed smooth.

  - Door leaves shall have top and bottom rails coped and welded to the jamb stiles.

  - Muntins (select from 1 and 2):

    - True Divided Lite muntins shall be coped and welded to the perimeter frame.  Muntin intersections shall be slotted, cross notched and welded.  All interior and exterior muntin joints shall be face welded and ground smooth.

    - Simulated Divided Lite Grids:

      - Hot-rolled exterior muntin - #84H profile shall be mitered or coped and fully back welded at all intersections.

      - Interior/exterior applied muntins - Profile shall be precut to meet perimeter frame. The intersections shall be milled to the extrusion profile. The muntin components shall be applied to the face of the glass with .045” VHB™ double adhesive tape after glazing.

  - Glazing

    - All doors shall be designed for inside or outside glazing.

    - Provide replaceable continuous glazing beads to suit the glass as specified.

    - Glazing beads shall be cut and shop fitted to each glass lite prior to shipment.

    - Manufacturer to provide correct glazing wedge and tape in accordance with the tested assembly.

- FACTORY FINISHING

  - Power of 5:

    - Cleaning:

      - All hot-rolled steel profiles must be acid pickled as defined by SSPC – SP8 to ensure a pristine, white metal substrate prior to fabrication.

    - Pretreatment:

      - Following welding and all machining operations, hot-rolled products and accessories are subjected to the following pretreatments geared specific to projects proximity to corrosive environment. Cold-rolled, formed sheet steel components are manufactured from A60 galvannealed sheet and subjected to applicable processes outlined below.

      - 12-stage process

        - Alkaline cleaning spray.

        - Alkaline cleaning submersion.

        - Water immersion rinse combo.

        - Water immersion rinse clean.

        - Acid immersion.

        - Neutralizing rinse.

        - Water immersion rinse clean.

        - Conditioner immersion.

        - Zinc phosphate immersion.

        - Rinse immersion.

        - Sealer immersion.

        - Water reverse osmosis rinse immersion.

3.     Epoxy E-coat Primer:

All pickled and pretreated frames and accessories are immersed into an electrostatic (E-coat) bath of PPG epoxy primer to ensure all substrates are encapsulated evenly and completely. Use of spray primers only will not be an acceptable alternative to this process due to benefits from additional cleaning and frame submersion.

- Permeate spray.

- Permeate rinse.

- Epoxy primer immersion and electrostatic encapsulation

- Water reverse osmosis rinse

- Oven-cure, 45 minutes @ 350° F

4.   Epoxy Powder Primer:

Following pre-treatments and E-coat system, all frames and accessories shall receive an abrasion resistant powder coating prior to final top-coat.

    - Powder is applied electrostatically over cured E-coat to a dry film thickness (DFT) of 2.0 – 3.0 mils.

    - Parts oven baked at 325° F to completely cure prior to final top coat.

    - Powder coat is intended as an intermediate finish applied prior to the final finish top coat.

5.   Polyester Powder Top Coat.

Following all pre-treatments, e-coat and powder abrasion layer, all products shall receive Hope’s ultrathane polyurethane finish with touch-up capability, low chalking and fading characteristics, unlimited color matching, and 70,000+ standard colors, including metallics.

6.   Power of 5 Overview:

    - Combined overall dry film thickness (DFT) shall be a minimum of 4.6 mils.

    - Overall process shall provide full documented compliance with the following criteria:

      - Acid Pickling:  SSPC-SP8.

      - Paint Blistering:  ASTM D714.

      - Humidity:  ASTM D4585.

      - Painted Products in Corrosive Environment:   ASTM D1654.

      - Salt Spray (Fog):  ASTM B117.

      - Cyclic Fog/Dry (Prohesion):  ASTM G85.

      - Salt Fog/UV Painted Metal:  ASTM D5894.

      - Pull Off Strength of Coating:  ASTM D4541.

PART 3 - EXECUTION

- INSPECTION

  - Door openings shall conform to details, dimensions and tolerances shown on the door manufacturers approved shop drawings.

  - Conditions which may adversely affect the door installation must be corrected before installation commences.

  - The wash down of the adjacent masonry or surrounding substrate must be completed before erection commences to prevent damage to the finish by the cleaning materials.

- INSTALLATION

  - Doors specified under this section shall be installed by experienced personnel.

  - Install doors in openings in strict accordance with approved shop drawings.

    - Set units plumb, level and true to line, without warp or rack of frames.

    - Anchor units securely to surrounding construction with approved fasteners.

    - The exterior joints between the doors, trim and mullions shall be properly sealed water-tight with an approved sealant and neatly pointed.

  - Attach door hardware, as required, and adjust doors to operate smoothly free from twist and to be weather-tight when closed.

  - Attach loose muntin grids per approved shop drawings, if applicable.

  - Repair any abraded areas of the factory finish.

- CLEANING

  - Door installer shall leave door surfaces clean after installation and ready to receive glass and glazing.  The door installer will not be responsible for final cleaning.