### PART 1 - GENERAL

- DESCRIPTION

  - Work included:

    - Roll-formed tubular steel impact approved double weatherstripped slide and fold door and frame configurations.

    - All door anchors, mullions, covers and trim.

    - Factory applied Hope’s Power of 5 Finishing System.

  - Related work specified elsewhere:

    - Glass, glazing and glazing materials, Section 08810.

    - Perimeter caulking, Section 07915.

    - Miscellaneous structural items, Section 05100.

- QUALITY ASSURANCE

  - Manufacturer shall have not less than 10 years experience in the fabrication of steel doors and be a member of The Steel Window Institute (SWI).

  - Installation of doors shall be done by experienced door installers.

  - Allowable tolerances: Size dimensions + 1/16 inch.

  - Source quality control:

    - Air infiltration test:

      - Air infiltration tested in accordance with ASTM E283 or Miami-Dade Testing Application Standard TAS 202 with maximum allowable air infiltration 0.3 CFM/SqFt. at 1.57 psf.

    - Water penetration test:

      - Water penetration test not required for FBC.  In High Velocity Hurricane Zone (HVHZ) areas, the doors can only be installed in locations protected by an overhang or canopy such that the included angle between the edge of the canopy or overhang to sill is less than or equal to 45 degrees.

    - Field test:

      - Field testing criteria (when applicable) shall be in accordance with AAMA 502-12.

    - Structural test

      - Static air pressure tested in accordance with ASTM E330 or Miami-Dade TAS 202 performed to a design load of 60 psf (positive and negative) and a structural load of 90 psf (positive and negative) while not exceeding the allowable deflection.

    - Forced entry test:

      - Meets or exceeds ASTM F588 or Miami-Dade TAS 202.

      - Grade 40 @ 300 pounds.

    - Impact test – Large missile:

      - Tested in accordance with ASTM E1996 or Miami-Dade TAS 202.

      - Withstand 2x4 missile impact at all designated contact points without penetration.

    - Cyclic wind loading test:

      - Tested in accordance with ASTM E1886 or Miami-Dade TAS 202.

      - No failure or distress after subjected to the cyclic sequence to a design load of 60psf (positive and negative).

    - Quality of Power of 5 finishing process shall meet or exceed the following designations:

      - Paint Blistering:  ASTM D714.

      - Humidity:  ASTM D4585.

      - Salt Spray (Fog):  ASTM B117.

      - Painted Products in Corrosive Environments:  ASTM D1654.

      - Cyclic Fog/Dry (Prohesion):  ASTM G85.

      - Slat Fog/UV Painted Metal:  ASTM D5894.

      - Pull off Strength of Coating:  ASTM D4541.

    - Upon request, the window manufacturer shall provide a test report from a qualified independent U.S. testing laboratory regularly engaged in testing windows to verify that products conform to test requirement as outlined.

- SUBMITTALS

  - Samples (as requested by architect):

    - Typical 6" long door profile with glazing beads.

    - Sample of specified muntin, showing welded intersections and glazing beads.

    - Color sample of finish.

    - Hardware.

  - Shop drawings and manufacturer's literature:

    - Submit for approval shop drawings showing door and installation details, including anchorage, fastening and recommended sealing methods.

    - Dimensioned elevations showing door opening and door sizes.

    - The manufacturer shall not commence any work until shop drawings have been approved.

    - Color charts for finishes.

- PRODUCT, STORAGE AND HANDLING

  - The General Contractor shall be responsible for the protection and storage of the doors after delivery to the site.

  - Store in designated areas in an upright position on wood slats or on a dry floor in a manner that will prevent damage.  Ventilate canvas or plastic coverings to prevent humidity buildup.

- WARRANTY

  - Provide Hope's standard 10 year Limited Warranty.

PART 2 - PRODUCT AND FABRICATION

- Manufacturers:

  - Furnish all labor and materials to complete the fabrication of doors and frames as shown on architect's drawings and as specified herein.  All doors and frames covered by this specification shall be domestically manufactured in the U.S.A.

  - Manufacturers:  Subject to compliance with requirements covered in this specification, provide products by Hope’s Windows, Inc. – Jamestown, NY (phone: 716-665-5124, e-mail: sales@hopeswindows.com) whose name and products are used to establish the standard of workmanship.

  - Substitutions:  Written approval necessary 10 days prior to bid through submission of the following:

    - Full-size window/door samples matching required scope.

    - Applicable test reports as outlined in Quality Assurance Section 1.2

    - List of (5) recently completed projects of similar size and scope.

- MATERIALS

  - Doors shall be manufactured from roll-formed 14 gauge galvanized steel tubular profiles.

  - Frames shall be manufactured from 12 gauge sheet steel.

  - Muntins (select from items 1 or 2 below):

    - True Divided Lite muntins:

      - Muntins shall be manufactured from solid hot-rolled steel, size to be determined by design.

      - Glazing rebate surfaces must be perpendicular to the stem of this profile.  Rebate surfaces that are tapered will not be acceptable.

      - 1-3/4” tee shall weigh 1.62 pounds per lineal foot, the 1-3/8” tee shall weigh 1.44 pounds per lineal foot and the 7/8” tee shall weigh 1.19 pounds per lineal foot (specify).

      - All steel muntin profiles must be a minimum of 1-3/4″ in depth.

    - Simulated Divided Lite muntins  (select from items below):

      - Hot-rolled stainless steel muntin - #84H profile shall be solid hot rolled from stainless steel with tapers rolled integral at the mill. #84H muntins shall be solidly welded to perimeter framing and dressed smooth. Opposite side muntin shall be extruded aluminum Alloy 6063-T5 matching the profiles as detailed.

      - Interior/exterior muntin - Profiles shall be extruded aluminum Alloy 6063-T5 matching the profiles as detailed.

  - Glazing beads shall be extruded aluminum alloy 6063-T5 with a minimum thickness of .062 inches.

  - Hardware reinforcements shall be 7, 10 or 12 gauge to suit specified hardware.

  - Power of 5 Finishing:

    - Cleaning

    - Pretreatment

    - Epoxy E-Coat primer

    - Epoxy powder primer

    - Ultrathane polyurethane top coat

- FABRICATION

  - Fabricate steel doors in accordance with approved shop drawings.

  - Corners of frame and ventilator shall be mitered or coped then solidly welded.  Exposed and contact surfaces shall be finished smooth flush with the adjacent surfaces.  All interior and exterior rail bar and muntin joints shall be face welded and ground smooth.

  - Subframe corners shall be coped and fully welded for maximum strength and weather tightness with face welds dressed smooth.

  - Muntins (select from 1 and 2):

    - True Divided Lite muntins shall be coped and welded to the perimeter frame.  Muntin intersections shall be slotted, cross notched and welded.  All interior and exterior muntin joints shall be face welded and ground smooth.

    - Simulated Divided Lite Grids:

      - Hot-rolled exterior muntin - #84H profile shall be mitered or coped and fully back welded at all intersections.

      - Interior/exterior applied muntins - Profile shall be precut to meet perimeter frame. The intersections shall be milled to the extrusion profile. The muntin components shall be applied to the face of the glass with .045” VHB™ double adhesive tape after glazing.

  - Anchoring shall be located at each hinge for maximum support.

  - Glazing:

    - All doors shall be designed for inside or outside glazing.

    - Provide replaceable continuous snap-in glazing beads to suit the glass as specified.

    - Glazing beads shall be cut and shop fitted to each glass lite prior to shipment.

    - Manufacturer to provide correct glazing wedge and tape in accordance with the tested assembly.

- FACTORY FINISHING

  - Power of 5:

    - Cleaning:

      - All hot-rolled steel profiles must be acid pickled as defined by SSPC – SP8 to ensure a pristine, white metal substrate prior to fabrication.

    - Pretreatment:

      - Following welding and all machining operations, hot-rolled products and accessories are subjected to the following pretreatments geared specific to projects proximity to corrosive environment. Cold-rolled, formed sheet steel components are manufactured from A60 galvannealed sheet and subjected to applicable processes outlined below.

      - 12-stage process

        - Alkaline cleaning spray.

        - Alkaline cleaning submersion.

        - Water immersion rinse combo.

        - Water immersion rinse clean.

        - Acid immersion.

        - Neutralizing rinse.

        - Water immersion rinse clean.

        - Conditioner immersion.

        - Zinc phosphate immersion.

        - Rinse immersion.

        - Sealer immersion.

        - Water reverse osmosis rinse immersion.

3.     Epoxy E-coat Primer:

All pickled and pretreated frames and accessories are immersed into an electrostatic (E-coat) bath of PPG epoxy primer to ensure all substrates are encapsulated evenly and completely. Use of spray primers only will not be an acceptable alternative to this process due to benefits from additional cleaning and frame submersion.

- Permeate spray.

- Permeate rinse.

- Epoxy primer immersion and electrostatic encapsulation

- Water reverse osmosis rinse

- Oven-cure, 45 minutes @ 350° F

4.   Epoxy Powder Primer:

Following pre-treatments and E-coat system, all frames and accessories shall receive an abrasion resistant powder coating prior to final top-coat.

    - Powder is applied electrostatically over cured E-coat to a dry film thickness (DFT) of 2.0 – 3.0 mils.

    - Parts oven baked at 325° F to completely cure prior to final top coat.

    - Powder coat is intended as an intermediate finish applied prior to the final finish top coat.

5.   Polyester Powder Top Coat.

Following all pre-treatments, e-coat and powder abrasion layer, all products shall receive Hope’s ultrathane polyurethane finish with touch-up capability, low chalking and fading characteristics, unlimited color matching, and 70,000+ standard colors, including metallics.

6.   Power of 5 Overview:

    - Combined overall dry film thickness (DFT) shall be a minimum of 4.6 mils

    - Overall process shall provide full documented compliance with the following criteria:

      - Acid Pickling:  SSPC-SP8.

      - Paint Blistering:  ASTM D714.

      - Humidity:  ASTM D4585.

      - Painted Products in Corrosive Environment:   ASTM D1654.

      - Salt Spray (Fog):  ASTM B117.

      - Cyclic Fog/Dry (Prohesion):  ASTM G85.

      - Salt Fog/UV Painted Metal:  ASTM D5894.

      - Pull Off Strength of Coating:  ASTM D4541.

- OPERABLE HARDWARE

  - Doors shall be hung on brass or stainless steel, 4-wheel concealed intermediate carrier located at the head and a brass or stainless steel, 2-wheel roller guides located at the sill.  The 4-wheel concealed intermediate carrier is constructed of two in-line rollers with ball-bearings.  The 2-wheel concealed intermediate carrier is self-aligning 2-wheel ball-bearing rollers.

  - Hinges shall be either brass or stainless steel, five-knuckle ball-bearing in both straight and offset configurations with quantities based on the door height.

  - Where required for opening or closing, certain hinges shall be equipped with a pull for hand operation.  The pull shall be furnished in either brass or stainless steel and finished to match the hinge.

  - Latching hardware shall be multipoint locking gears with lever handle trim for interior and exterior operation requiring a 10 and 12 gauge steel lock stile.  Trim shall be either rose or escutcheon and the lock shall be an entrance function with lever handles both sides, key cylinder exterior and thumbturn interior

  - All leaves shall be fitted with surface applied top and bottom bolts.  The bottom bolt is 8” long and the top bolt is determined by the height of the door and shall be key lockable.

  - Thresholds shall be aluminum alloy 6063-T5 and designed to accept the 2-wheel roller guides.

  - Head track shall be aluminum alloy 6063-T5 and designed to accept the 4-wheel concealed intermediate carrier.

  - Weatherstripping shall be extruded vinyl, EPDM closed cell sponge, flexible silicone or polyethylene clad urethane foam.

PART 3 - EXECUTION

- INSPECTION

  - Door openings shall conform with details, dimensions and tolerances shown on the door manufacturer's approved shop drawings.

  - Conditions which may adversely affect the door installation must be corrected before installation commences.

  - The wash down of the adjacent masonry or surrounding substrate must be completed before erection commences to prevent damage to the finish by the cleaning materials.

- INSTALLATION

  - Doors specified under this section shall be installed by experienced personnel.

  - Install doors in openings in strict accordance with approved shop drawings.

    - Set units plumb, level and true to line, without warp or rack of frames.

    - Anchor units securely to surrounding construction with approved fasteners.

    - The exterior joints between the doors, trim and mullions shall be properly sealed watertight with an approved sealant and neatly pointed.

  - Attach door hardware, as required, and adjust doors to operate smoothly free from twist and to be weathertight when closed.

  - Attach loose muntin grids per approved shop drawings, if applicable.

  - Repair any abraded areas of the factory finish.

- CLEANING

  - Door installer shall leave door surfaces clean after installation and ready to receive glass and glazing.  The door installer will not be responsible for final cleaning.