### PART 1 - GENERAL

- DESCRIPTION

  - Work included:

    - Hot-rolled steel double weatherstripped fire rated swing door configurations.

    - All fire rated door anchors, mullions, covers and trim.

    - Factory applied Hope’s Power of 5 Finishing System.

  - Related work specified elsewhere:

    - Glass, glazing and glazing materials, Section 08810.

    - Perimeter caulking, Section 07915.

    - Miscellaneous structural items, Section 05100.

- QUALITY ASSURANCE

  - Manufacturer shall have not less than 10 years experience in the fabrication of heavy custom steel doors and be a member of The Steel Window Institute (SWI).

  - Installation of doors shall be done by experienced door installers.

  - Allowable tolerances: Size dimensions + 1/16 inch.

  - Source quality control:

    - Labeled Fire Rating:

      - Positive Pressure Tested to NFPA 252(1995), UBC 7-2-1997, UL 10c, ASTM E 2010-99, and CAN4 S104.

      - Door Size Capabilities:

        - Single up to 3’6” x 8’0”.

        - Pair up to 7’ 0” x 8’ 0”.

      - Combined Door Frame with Integral Glazed Transom – maximum size 84” wide x 131” high.

      - Glass Size in Door: Maximum area is 1,755 square inches, maximum height is 47-11/16”, and maximum width is 36-13/16”.  Note – These glass sizes are based on Hope’s maximum sizes. Other listed glass products can be used and the maximum size limitations will be determined by the lesser of the two components: Hope’s framing above or the glass (see manufacturer).

      - Each fire rated door & frame assembly shall be furnished with a Warnock Hersey certification label, self adhesive mylar. The label shall be located at the hinge jamb of the frame, visible when door is open.

    - Air infiltration test:

      - Products must be independently lab tested and meet or exceed ASTM E283.

      - Maximum air infiltration 0.30 CFM/SQ Ft. with differential pressure across window unit of 1.57/ 6.24 PSF.

    - Water penetration test:

      - Products must be independently lab tested and meet or exceed ASTM E331.

      - No water penetration for 15 minutes when window is subjected to a rate of flow of 5 gal./hr./sq. ft. with differential pressure across window unit of 4.50.

    - Field test:

      - Field testing criteria (when applicable) shall be in accordance with AAMA 502-12

    - Structural test:

      - Meets or exceeds ASTM E330.

    - Quality of Power of 5 non-coastal finishing process shall meet or exceed the following designations (non-coastal application – greater than (1) mile from salt water and/or similar corrosive  environments):

      - Paint Blistering:  ASTM D714.

      - Humidity:  ASTM D4585.

      - Salt Spray (Fog):  ASTM B117.

      - Painted Products in Corrosive Environments:  ASTM D1654.

      - Cyclic Fog/Dry (Prohesion):  ASTM G85.

      - Slat Fog/UV Painted Metal:  ASTM D5894.

      - Pull off Strength of Coating:  ASTM D4541.

    - Quality of Power of 5 coastal finishing process shall meet or exceed the following designations (Coastal application – less than (1) mile from salt water and/or similar corrosive environments):

      - Acid Pickling:  SSCP-SP8.

      - Hot Dip Galvanize:  ASTM A123.

      - Adhesion:  ASTM D3359, no loss.

      - Hardness:  ASTM D3363 (pencil), H min.

      - Salt Spray:  ASTM B117, passes 3000 hrs.

      - Humidity:  ASTM D2247, 3000 hours, few #8 blisters.

      - Impact Resistance (3mm):  ASTM D2794, no loss.

      - Color Retention:  ASTM D2244, 5 year less than or equal to 5 delta E.

      - Chalk Resistance:  ASTM D4214, #8 rating.

      - Gloss Retention:  ASTM D523, greater than or equal to 30 percent retention.

    - Upon request, the window manufacturer shall provide a test report from a qualified independent U.S. testing laboratory regularly engaged in testing windows to verify that products conform to test requirement as outlined.

- SUBMITTALS

  - Samples (as requested by architect):

    - Typical door 6" long profile with glazing beads.

    - Sample of specified muntin, showing welded intersections and glazing beads.

    - Color sample of finish.

    - Hardware.

  - Shop drawings and manufacturer's literature:

    - Submit for approval shop drawings showing door and installation details, including anchorage, fastening and recommended sealing methods.

    - Dimensioned elevations showing door opening and door sizes.

    - The manufacturer shall not commence any work until shop drawings have been approved.

    - Color charts for finishes.

- PRODUCT, STORAGE AND HANDLING

  - The General Contractor shall be responsible for the protection and storage of the doors after delivery to the site.

  - Store in designated areas in an upright position on wood slats or on a dry floor in a manner that will prevent damage.  Ventilate canvas or plastic coverings to prevent humidity buildup.

- WARRANTY

  - Provide Hope’s standard 10 year Limited Warranty.

PART 2 - PRODUCT AND FABRICATION

- Manufacturers:

  - Furnish all labor and materials to complete the fabrication of doors as shown on architect's drawings and as specified herein.  All doors covered by this specification shall be domestically manufactured in the U.S.A.

  - Manufacturers:  Subject to compliance with requirements covered in this specification, provide products by Hope’s Windows, Inc. – Jamestown, NY (phone: 716-665-5124, e-mail: sales@hopeswindows.com) whose name and products are used to establish the standard of workmanship.

  - Substitutions:  Written approval necessary 10 days prior to bid through submission of the following:

    - Full-size window/door samples matching required scope.

    - Applicable test reports as outlined in Quality Assurance Section 1.2

    - List of (5) recently completed projects of similar size and scope.

- MATERIALS

  - Heavy custom double weatherstripped doors shall be manufactured from solid hot-rolled steel profiles.

    - Profiles made from steel with flanges rolled integrally at the mill.

    - Perimeter frames and ventilator profiles shall have glazing rebates providing an unobstructed glazing surface of at least 3/4".

    - Glazing rebate surfaces must be perpendicular to the web or stem of the profile.  Applied glazing rebate extensions and rebate surfaces that are tapered will not be acceptable.

    - Combined weight of frame and ventilator profiles shall be a minimum of 4.20 pounds per lineal foot. Frame section alone shall not weigh less than 1.80 pounds per lineal foot.

    - All steel profiles must be a minimum of 1-3/4″ in depth.

    - The frame and ventilator profiles shall have integral grooves located in the exterior and interior bedding contacts for the reception of double weatherstripping.

    - Lockboxes and lockstiles shall incorporate both custom formed profiles and hot-rolled section as shown on the shop drawings and welded to the door leaf

    - Kickpanels shall be made from two, 16 gauge sheet steel panels with a rigid polyisocyanurate insulation core.

  - Muntins:

    - Steel tee muntins shall be manufactured from hot rolled steel, size to be determined by design.

    - Glazing rebate surfaces must be perpendicular to the stem of this section.  Rebate surfaces that are tapered will not be acceptable.

    - The 175M muntin shall weigh 2.20 pounds per lineal foot, the 1-3/4” tee shall weigh 1.62 pounds per lineal foot and the 1-3/8” tee shall weigh 1.44 pounds per lineal foot.

  - Glazing beads shall be cold formed from a minimum of 14 gauge galvanized steel.

  - Weatherstripping shall be from extruded vinyl, EPDM closed cell sponge, flexible silicone or polyethylene clad urethane foam.

  - Mullions:

    - Openings may be divided by approved mullions anchored at both ends. Mullions can be plate, tube, and flat type per certified details. Right angle and other corner mullions are also available. Mullions shall be selected to comply with stated widow loading criteria per specifications.

  - All screws that are furnished by Hope’s for hardware, trim, covers, anchoring, weatherbars, water dams, screens, etc. shall be non-ferrous brass or stainless steel.  Glazing bead screws are plated steel.

  - Power of 5 Finishing  (Select from item #1 for non-coastal applications or from item #2 for coastal applications):

    - Non-Coastal – greater than (1) mile from salt water and/or similar corrosive environments.

      - Cleaning.

      - Pretreatment.

      - Epoxy E-Coat primer.

      - Epoxy powder primer.

      - Ultrathane polyurethane top coat.

    - Coastal – within (1) mile of salt water and/or similar corrosive environments.

      - Cleaning.

      - Pretreatment.

      - Brush-Off Blast Cleaning.

      - Epoxy Powder Primer.

      - Polyester Powder Top Coat or Ultrathane polyurethane Top Coat.

- FABRICATION

  - Fabricate steel doors in accordance with approved shop drawings.

  - Corners of frame and ventilator shall be mitered or coped then solidly welded.  Exposed and contact surfaces shall be finished smooth flush with the adjacent surfaces.  All interior and exterior rail bar and muntin joints shall be face welded and ground smooth.

  - Lock boxes and lock stiles shall incorporate both custom formed profiles and hot-rolled section as shown on the shop drawings and welded to the door leaf.

  - Steel tee muntins shall be tenoned and welded to the perimeter frame.  Muntin intersections shall be slotted, cross notched and welded.  All interior and exterior muntin joints shall be face welded and ground smooth.

  - Glazing:

    - All doors shall be designed for inside or outside glazing.

    - Provide replaceable continuous screw on glazing beads to suit the fire rated glass specified.

    - Glazing beads shall be cut and shop fitted to each glass lite prior to shipment.

    - Glazing beads are available to accommodate a variety of fire rated glazing materials 3/16” through 1-5/16” (certain materials have size limits that need to be considered).

    - Glazing accessories to be per manufacturer of tested glazing materials.  Exterior applications should have cap bead of an approved silicone for weather resistance.

  - Weatherstrip:

    - All door leaves shall receive continuous double vinyl weatherstripping that shall be applied to the integral weatherstrip grooves in the interior and exterior contact surfaces of the head and jambs of the frame and door sections.  Weatherstripping that is surface applied or requires additional retainer or requires screws for application shall not be acceptable.  Sill weatherstripping shall be:

      - Surface applied to the face of the door.

      - Applied to an integral T-slot in the threshold.

      - Attached to the underside of the door.

  - Labeling:

    - Each fire rated door shall be furnished with a Warnock Hersey® certification label, self adhesive Mylar. The label shall be located at the inside sill of the door.

- FACTORY FINISHING (Select from items A or B below)

  - Power of 5 (non-coastal):

    - Cleaning:

      - All hot-rolled steel profiles must be acid pickled as defined by SSPC – SP8 to ensure a pristine, white metal substrate prior to fabrication.

    - Pretreatment:

      - Following welding and all machining operations, hot-rolled products and accessories are subjected to the following pretreatments geared specific to projects proximity to corrosive environment. Cold-rolled, formed sheet steel components are manufactured from A60 galvannealed sheet and subjected to applicable processes outlined below.

      - Inland locations (12-stage process) – Greater than one (1) mile from salt water and/or similar corrosive environments.

        - Alkaline cleaning spray.

        - Alkaline cleaning submersion.

        - Water immersion rinse combo.

        - Water immersion rinse clean.

        - Acid immersion.

        - Neutralizing rinse.

        - Water immersion rinse clean.

        - Conditioner immersion.

        - Zinc phosphate immersion.

        - Rinse immersion.

        - Sealer immersion.

        - Water reverse osmosis rinse immersion.

3.     Epoxy E-coat Primer:

All pickled and pretreated frames and accessories are immersed into an electrostatic (E-coat) bath of PPG epoxy primer to ensure all substrates are encapsulated evenly and completely. Use of spray primers only will not be an acceptable alternative to this process due to benefits from additional cleaning and frame submersion.

- Permeate spray.

- Permeate rinse.

- Epoxy primer immersion and electrostatic encapsulation

- Water reverse osmosis rinse

- Oven-cure, 45 minutes @ 350° F

4.   Epoxy Powder Primer:

Following pre-treatments and E-coat system, all frames and accessories shall receive an abrasion resistant powder coating prior to final top-coat.

    - Powder is applied electrostatically over cured E-coat to a dry film thickness (DFT) of 2.0 – 3.0 mils.

    - Parts oven baked at 325° F to completely cure prior to final top coat.

    - Powder coat is intended as an intermediate finish applied prior to the final finish top coat.

5.   Polyester Powder Top Coat.

Following all pre-treatments, e-coat and powder abrasion layer, all products shall receive Hope’s ultrathane polyurethane finish with touch-up capability, low chalking and fading characteristics, unlimited color matching, and 70,000+ standard colors, including metallics.

6.   Power of 5 Overview (non-coastal):

    - Combined overall dry film thickness (DFT) shall be a minimum of 4.6 mils (inland locations)

    - Overall process shall provide full documented compliance with the following criteria:

      - Acid Pickling:  SSPC-SP8.

      - Paint Blistering:  ASTM D714.

      - Humidity:  ASTM D4585.

      - Painted Products in Corrosive Environment:   ASTM D1654.

      - Salt Spray (Fog):  ASTM B117.

      - Cyclic Fog/Dry (Prohesion):  ASTM G85.

      - Salt Fog/UV Painted Metal:  ASTM D5894.

      - Pull Off Strength of Coating:  ASTM D4541.

  - Power of 5 (coastal):

    - Cleaning:

All hot-rolled steel profiles must be acid pickled to white metal as defined by SSPC – SP8 creating a pristine, white metal substrate which is paramount to achieving ultimate finish performance.

    - Pretreatment:

Following welding and all machining operations, hot-rolled products and accessories are subjected to the following pretreatment process.

      - Hot-Dip Galvanize.

      - Parts are cleaned and immersed in a molten pool of pure zinc per ASTM A123 to create a dry film       thickness (DFT) of 4 – 8 mils of cathodic protection.

      - Quality Control.

      - Mechanical Cleaning.

    - Brush-Off Blast Cleaning:

      - Galvanized parts shall be brush-off blast cleaned in accordance with SSPS-SP16 to profile surface prior to primer application.

      - All Parts shall be oven heated prior to finishing to prevent outgassing through epoxy primer.

    - Epoxy Powder Primer:

Following pretreatment and brush-off blast cleaning all parts shall receive an abrasion resistant epoxy powder coat to ensure ultimate substrate protection. Epoxy powder primer is intended as an intermediate finish applied prior to the final finish top coat.

      - Within 12 hours of hot-dip galvanizing pretreatment all frames and accessories shall receive an epoxy powder primer for abrasion resistance.

      - After hot-dip galvanizing has been cleaned, brush-off blasted, and oven outgassed – epoxy powder primer is applied electrostatically to a dry film thickness (DFT) of 2.0 – 4.0 mils.

      - Parts are oven baked in preparation of top coat application.

    - Polyester Powder Top Coat or Ultrathane Polyurethane Top Coat:

The top coat defines the final stage to the overall aesthetics and performance of the finished product.

        - Polyester powder top coat shall be applied immediately over epoxy powder primer.

        - Powder top coat is electrostatically applied to a dry film thickness (DFT) of 2.0 – 4.0 mils.

        - Parts are oven baked to fully cure.

    - Power of 5 Overview (coastal):

      - Combined overall dry film thickness (DFT) of hot-dip galvanizing, epoxy primer, and polyester powder top coat or Ultrathane Polyurethane Top Coat shall be between 8.0 – 16.0 mils.

      - Overall process shall provide full documented compliance with the following criteria (as applicable):

        - Acid Pickling:  SSCP-SP8.

        - Hot Dip Galvanize:  ASTM A123.

        - Adhesion:  ASTM D3359, no loss.

        - Hardness:  ASTM D3363 (pencil), H min.

        - Salt Spray:  ASTMB 117, passes 3000 hrs.

        - Humidity:  ASTM D2247, 3000 hours, few #8 blisters.

        - Impact Resistance (3mm):  ASTM D2794, no loss.

        - Color Retention:  ASTM D2244, 5 year less than or equal to 5 delta E.

        - Chalk Resistance:  ASTM D4214, #8 rating.

        - Gloss Retention: ASTM D 523, greater than or equal to 30 percent retention.

- OPERABLE HARDWARE

  - Single Door or Active Leaf of Pair:

    - Doors shall be hung on (3) 4” x 2-5/16”x .130” steel ball bearing hinges at the jamb.

    - Provide fire rated mortise lock with 2-3/4” backset and latch bolt with minimum of 3/4” throw.  Lock trim as specified by architect.

    - Provide two concealed expansion lugs at both hinge and latch jambs.

    - Provide surface mounted fire rated closer. Hold open feature is not permitted.

    - Doors shall be hung and hardware shall be fitted prior to shipment, however some surface mounted hardware may be removed and shipped loose for field attachment.

  - Inactive Leaf of Pair:

    - Doors shall be hung on (3) 4” x 2 5/16” x .130” steel ball bearing hinges at the hinge jamb.

    - Provide fire rated surface bolts at head & sill rails.

    - Closers are not required on inactive leaf.

    - Provide two expansion lugs on concealed at hinge jamb.

    - Hardware shall be shipped loose for field application, however doors shall be hung and hardware fitted prior to shipment.

  - Thresholds

    - Threshold shall be as shown (select material from items a or b):

      - Aluminum (powder coated).

      - Bronze (toned US10B or Bead Blast mill finish).

PART 3 - EXECUTION

- INSPECTION

  - Door openings shall conform to details, dimensions and tolerances shown on the door manufacturers approved shop drawings.

  - Conditions which may adversely affect the door installation must be corrected before installation commences.

  - The wash down of the adjacent masonry or surrounding substrate must be completed before erection commences to prevent damage to the finish by the cleaning materials.

- INSTALLATION

  - Doors specified under this section shall be installed by experienced personnel.

  - Install doors in openings in strict accordance with approved shop drawings.

    - Set units plumb, level and true to line, without warp or rack of frames.

    - Anchor units securely to surrounding construction with approved fasteners.

    - The exterior joints between the doors, trim and mullions shall be properly sealed water-tight with an approved sealant and neatly pointed.

  - Attach door hardware, as required, and adjust doors to operate smoothly free from twist and to be weather-tight when closed.

  - Repair any abraded areas of the factory finish.

- CLEANING

  - Door installer shall leave door surfaces clean after installation and ready to receive glass and glazing.  The door installer will not be responsible for final cleaning.